Street Furniture Maintenance Manual

Care and maintenance of the street furniture are carried out depending on materials used in the product and the protective coating applied to its surface.

Commonly used materials and finishes

- Carbon steel, hot-dip galvanised and painted.

- Stainless steel, grade AISI304, grit 320 or polished. Grade AISI316 available on demand.

- Wood – Northern spruce slats, varnished.

Influence of environmental conditions

- UV rays from the Sun diminish the protective layer and colour pigment of the surface.

- Humidity oscillations result in swelling and shrinking of the wood and cracks may appear. Under lasting conditions of humidity, mould may develop.

- Hail and snow may act as an abrasion to the coating.

- Temperature fluctuations like heat from direct sun rays may result in forming cracks on wooden surfaces.

- Sand–salt (NaCl) mixture and other chemicals used for roads’ maintenance may also act as a corrosive agent damaging surface or a protective layer of the material.

Care and maintenence

- A long-lasting stack of melting snow on the horizontal wooden surfaces, e.g., on bench seats should be removed.

- Once a year after winter a visual inspection of the wooden surface should be carried out. In case a protective layer is damaged and/or cracks have appeared restoration of the wooden protective layer should be performed according to Wooden Surface Restoration Guide.

- Sand-salt mixture and other aggressive chemicals close to street furniture should be spread with care avoiding direct contact. Salt crystals should be cleaned off by spraying and wiping with a cloth and a neutral or slightly alkaline water solution (pH 8-10).

- Stainless steel generally has a low-maintanence surface but for sanded surfaces exposed to contaminated urban, industrial or coastal areas it is recommended to apply a protective solution to achieve a shiny appearance and avoid stains. The surface forms a protective coat by spraying, rubbing and polishing the solution with a dry microfibre cloth.

The expected lifecycle

The life cycle of street furniture depends on environmental conditions and the maintenance carried out. Proper attention should be paid to wooden surfaces by following the Wooden Surface Restoration Guide downloadable at www.metaldarbnica.lv

Effecting proper maintenance usually exceeds the lifetime of street furniture to more than ten years.