Maintenance – metal surfaces

Street Furniture Maintenance Manual: Metal Surfaces

Care and maintenance of urban furniture depends on a combination of factors: what materials are used in the product, what kind of protective coating is applied, and what environmental conditions impact the furniture.

Materials and finishes options used in the product:

- Carbon steel galvanised – the most robust kind of coating, resistant to all kinds of outdoor impacts.

- Carbon steel galvanised and painted – ensuring long-lasting outdoor durability and esthetic appearance.

- Stainless steel, grade AISI304 sanded G320 – has a semi-shiny look and is suited for extensively used spaces. Not recommended in polluted and coastal areas

- Stainless steel, grade AISI304 bead-blasted – has a semi-matt look, can hardly be damaged or scratched, and is robust in aggressive environments.

Influence of environmental conditions on urban furniture:

- UV rays from the Sun diminish the surface protective layer, especially for coatings containing lesser colour pigment.

- Humidity and temperature fluctuations may result in swelling and shrinking of softwood and cracks may appear. Under lasting conditions of humidity, mould may develop.

- Hail and snow may act as an abrasion to the coating.

- Sand–salt (NaCl) mixture and other chemicals used for road maintenance may act as a corrosive agent damaging material and a protective layer.

- Polluted air with sulphur dioxide or nitrogen oxides turns into acid in water or humid environments.

- Ocean and sea coastal areas are influenced by ‘flying’ salt particles, making the environment particularly aggressive.

Care and maintenance:

- Prevent prolonged contact of snow drifts with street furniture, especially to ensure that wet snow does not accumulate, by regularly cleaning it;

- Avoid the use of sand-salt mixtures, as well as other chemically aggressive chemical care products on the sidewalk near street furniture as much as possible;

- At least once a year, it is necessary to visually assess the condition of metal parts and, if necessary, wash the surface of the metal coating using a neutral detergent. Water or a weakly alkaline solution (pH 8-10) is sprayed onto the metal surface and wiped with a clean, dry cloth in circular motions.

- Stainless steel generally has a low-maintenance surface but for sanded surfaces exposed to contaminated urban, industrial or coastal areas it is recommended to apply a protective solution to achieve a shiny appearance and avoid stains. The surface forms a protective coat by spraying, rubbing and polishing the solution with a dry microfibre cloth.

The expected lifecycle

The life cycle of street furniture depends on environmental conditions and the maintenance carried out. Effecting proper maintenance usually exceeds the lifetime of street furniture by more than ten years.

For more information contact us: info@metalfabrik.eu